Date of issue:

Issued by:

# DuoBat 120+ System                                 5 pages

# NBS SPECIFICATION K21 CLAUSE 130

Project:				•

### BATTENED TIMBER FLOORING FLOATING FLOOR

Location:				•

Base and Preparation:	• New or (Delete as necessary) Existing concrete floor flooring to conform to BS8204 Part 1 2003, to be flatness tolerance SR3, with a smooth finish having a suitable damp proof membrane underneath.

• If block and beam suspended ground floor construction, ensure that the void is correctly ventilated to current Building Regulations with any earth base at least 225mm below any pre cast beams

• As clause 260.

Batten System:	•Junckers DuoBat 120+ double batten system, comprising a laminated spruce veneered 25mm deep by 60mm wide top batten mounted with 12mm rubber pads at 400mm centres, to be clicked into “J Lock” elements, and a 40mm x 39mm laminated spruce veneered lower batten mounted with Junckers “J Lock” elements at 336mm centres.  Upper battens to be set out at 336mm centres and to have factory produced leaf joints at all ends.  Lower battens to be set out at 400mm centres and have J Lock adjustable wedges fixed at 673mm centres along the lower battens .

Junckers Gable Battens to be installed at all perimeters. Junckers start battens to be used as first row of battens to ensure correct setting out of the system.

•  All to be packed to a surface tolerance flatness of no more than a 3mm gap showing under a 3m straight edge. Ensure that any packing used is secured to the plywood packing areas.

• All conforming to BS8201 and BSEN14904:2006 Area A4.

• Load bearing capacity 5.0kN/m2. For information on retractable seating loadings contact Junckers.

• Note:  Minimum height of system to be 120mm.

• As clause 325.

Thermal Insulation		• If required

between Battens:

Moisture Membrane:		• Junckers Sylvathene installed under battens and on

top of the cementitious base.

• As clause 310.

Boards:	• Junckers BREEAM A+ rated Solid Pre-finished hardwood, free from decay and insect attack and PEFC certified.  Planed all round.

Consisting of two rows of staves with unique double dovetail construction.

• Polyback, polythene or lacquer moisture balancer fitted to the underside.

Manufacturer:                              • Junckers Ltd

1 Wheaton Road, Witham, Essex, CM8 3UJ

Tel No 0044 1376 534737

E mail sales@junckers.co.uk

Web www.junckers.co.uk

Area manager contact – ........................

Tel No .............................

Species:		• Solid press dried Beech

Grade:		•. SylvaSport Premium or (Delete as necessary)

Club or (Delete as necessary) SylvaTech plus

Premium or (Delete as  necessary) Club

Finished Face Width:		•   129mm.

Finished Thickness:		•   22mm.

Finished Length:		•  3700mm.

Edges:	• Tongue and grooved.  Square edged and wax edged sealed.

Moisture Content		• 7.5% + manufacturing tolerance.

at Time of Fixing:

Fixing:	•  By secret nailing using 50mm – 65mm lost head nails or 50mm Portanails or 2.5mm diameter Pneumatic nails to each batten to each batten using a modified MAX pneumatic nail gun.

• Floor to be installed to a 10 board measure of…………cm, (using Junckers 0.2mm, 0.4mm, 0.6mm or 0.8mm (Delete as necessary) spacers between each board) to suit the expected relative humidity range of 35-65%RH of the building when in use.

• 10 board measure to be………….cm

• All laid to manufacturer’s recommendations.

• As clause 350.

Finish:	• Factory finished with several coats of UV light cured lacquer and one coat of Junckers two-component polyurethane Isolacquer, total film thickness 45 microns.

Accessories:	• Junckers 38mm x 48mm combi skirting boards.

• Junckers Bushings at post hole locations

Other Requirements:	• Line marking to be carried out using Junckers HP SportsLine paint.

• Apply one coat of Junckers HP Sport lacquer on completion of line marking.

210		 WORKMANSHIP GENERALLY:

•   Keep boards dry before installation.

• Methods of fixing and fasteners to be as section Z20 unless specified otherwise.

• Protect from dirt, stains and damage until Practical Completion using suitable coverings and boards laid as the work proceeds.

220					ENVIRONMENT:

• Do not start work specified in this section before the building is weather tight, wet trades have finished their work and the building is well dried out.

• Before, during and after laying, temperature and humidity must be maintained at levels approximating to those which will prevail after building is occupied.

•• Relative humidity must be maintained within the range of 35-65%RH. This must be provided prior to installation and maintained from there on.

Exchange of Information

Ensure that there is a system in place for proper exchange of information between the design team and all specialist contractors, including persons responsible for commissioning and hand over, to ensure that the correct environmental conditions are achieved and maintained.

- HEATING:

• Agree arrangements for operating the heating installation up to the date of Practical Completion of the Works to ensure that excessive moisture movement of flooring does not take place.

• The heating system has been designed to provide ………………. heating giving air temperatures in the range …………...°C  to……………ºC.

- AIR CONDITIONING:

• Agree arrangements for operating the air conditioning installation up to the date of Practical Completion of the Works to ensure that excessive moisture movement of flooring does not take place.

• The system has been designed to provide ……………….……………………………………………..

- FIXTURES:

Do not start work specified in this section until any fixtures around which flooring is to be fixed have been installed.

- MOISTURE CONTENT OF BASE:

Where flooring is to be laid on a new or existing concrete or screed base:

• Ensure that drying aids have been turned off for not less than 4 days, then

• Test for moisture content using an accurately calibrated hygrometer in accordance with BS8201, Appendix A.

•   Take readings in all corners, along edges, and at various points over the area being tested.

•   Do not lay flooring until all readings show 75% relative humidity or less.

- MOISTURE CONTENT OF TIMBER:

When instructed by CA, test timber with an approved moisture meter to manufacturer’s recommendations. Provide CA with records all tests and results.

- CONTROL SAMPLE:

Complete sample area, being part of the finished work, in approved location as follows and obtain approval of appearance before proceeding:

Clause reference:……………………..

Location:………………………………

Size:……………………………………

Include features:………………………

310		VAPOUR CHECK/MOISTURE MEMBRANE:

• To be lapped and taped, and turned up at perimeter walls.

• Ensure membrane is clean, dry and free from punctures and tears before laying flooring.

- FLOORING BATTENS:

• Free from decay and active insect attack, and with no knots wider than half the width of the section.

• Regularised.

• Moisture content at time of installation 12-14%.

- FIXING BOARDS:

• Fix each board securely to give a flat true surface free from undulations, hammer marks, scratches and protruding fastenings.

• Allow for movement of timber through expansion or contraction by installing to manufacturer’s recommendations to suit the expected relative humidity range of building when in use.

• Header joints to be tongue and grooved, tightly butted and positioned centrally over supports.

• Unless otherwise instructed surface nail first and last rows of boards.  Punch nails below surface and stop with filler, as recommended by flooring manufacturer.

•   Header joints to be uniformly positioned to a 1008mm staggered pattern across the floor.

- EXPANSION PROVISION:

• Expansion gaps:

• Edges of flooring: Parallel to lie of boards form a clear perimeter gap equivalent to 1.5mm per running metre width of flooring on either side and around pipes, columns etc. minimum size 15mm and to be covered by  Junckers combi skirting board 38mm x 48mm.

• Ends of flooring: A gap equivalent to 1mm per running metre length of flooring to be left at either end of the flooring, minimum size 15mm.

• Intermediate expansion joints: Floor to be installed to a 10 board measure of…………cm,  (using Junckers 0.2mm, 0.4mm, 0.6mm or 0.8mm (Delete as necessary) PVC spacers between each board) to suit the expected relative humidity range of 35-65%RH of the building when in use.

• Remove any temporary spacer blocks and debris

before fixing skirting/cover fillets